## Slide 1: 5-Week Research Update: Fun with Glass!
Jackie Loven
10 July 2017

## Slide 2: Recall
Crack fraction: total cracks/ total indentation corners
Hardness: load/ observed area of indent
Crack threshold: load at which cracks appear
Pileup: plastically deformed material pushed up around indent

## Slide 3: Current Problems
Calcium aluminosilicates aren’t that well characterized
  fracture properties
  hardness
  But these test measurements are super subjective

## Slide 4: Recent Projects
Taking measurements
  crack fraction
  hardness
  crack threshold over time
  pileup
Characterizing error in measurements
Making indent edges clearer

## Slide 5: Collecting Data

## Slide 6: Initial observations
Caila’s data from last year:

## Slide 7: Initial observations
My data was very different

## Slide 8: The Culprit: Surface Roughness?
3 Samples
  0.05 µm polish
  0.5 µm polish
  1 µm polish
Roughness data from profiles
  Caila’s samples: Looked inconclusive (actual: 1 µm polish)
  My samples: Confirmed 0.5 µm polish level

## Slide 9: The Culprit: Surface Roughness?
Roughness changes crack fraction

## Slide 10: Also The Culprit: Time?
Samples photographed immediately after indenting and after 1 week

## Slide 11: The Culprit: Time?
Before:

## Slide 12: The Culprit: Time?
After: cracks appear over time

## Slide 13: Sample Differences
Time: affects crack threshold
Surface polish level: affects cracks but not hardness

## Slide 14: Quantifying Error

## Slide 15: Laser Profiler Error
Laser profiler can’t measure small indents, pileup
AFM should show what small indents and pileup actually look like
  A linear correction factor between laser profiler and AFM would be fantastic

## Slide 16: AFM Results
Currently analyzing results and comparing to laser profiler

## Slide 17: Making Indent Edges Clearer

## Slide 18: Traditional Hardness Error
Indents in metal samples are gorgeous. Ours? Not so much.
vs.

## Slide 19: Traditional Hardness Error
For small indents/ groups without a laser profiler:
  Indent measurements are super subjective
  Can we make measurements easier?

## Slide 20: Traditional Hardness Error
Make the samples look like metal
Carbon and gold didn’t work too well, but gold-palladium is great

## Slide 21: Future Work
Analyze AFM data
Make software usable and available to public
Take nice images of coated indents, see how much the coating changes the programatically determined area

## Slide 22: Future Work
Analyze AFM data
Make software usable and available to public
Take nice images of coated indents, see how much the coating changes the programatically determined area
~~**~~ write all the papers ~~**~~

## Slide 23: Questions